## Slide 1
Structure of Crystalline Solids

## Slide 2
Crystalline materials: Unit Cell
For the face centered cubic crystal structure (a) a hard sphere unit cell representation
(b) a reduced-sphere unit cell
(c) an aggregate of many atoms.
When describing crystalline structures, atoms (or ions) are thought of as being solid spheres having well-defined diameters. This is termed the atomic hard-sphere model in which spheres representing nearest-neighbor atoms touch one another
Unit Cell: The basic structural unit of a crystal structure. Its geometry and atomic positions
define the crystal structure.

## Slide 3
Unit cells and unit vectors
Lattice parameters=
axial lengths: a, b, c
interaxial angles: α, β, γ

## Slide 5
Two other important characteristics of a crystal structure:
Coordination number : the total number of nearest neighbor atoms
Atomic packing factor (APF): the fraction of volume in a crystal structure that is occupied by atoms.
• Coordination # = 6
(# nearest neighbors)
For metals, each atom has the same number of nearest-neighbor or touching atoms, which is the coordination number
Simple Cubic Structure

## Slide 6: Atomic Packing Factor (APF)
• APF for a simple cubic structure = 0.52
APF =
a
3
4
3

(0.5a)
3
1
atoms
unit cell
atom
volume
unit cell
volume
close-packed directions
a
R=0.5a
contains 8 x 1/8 =
1
atom/unit cell
unit cell length=a
atomic radius=R
Simple Cubic Structure
8 atoms but each atom is
shared by 8 unit cells.
→ 1 atom per unit cell

## Slide 7
Bravais Lattices in 3-dimension

## Slide 8
The atomic bonding in this group of materials is metallic and thus nondirectional in nature.
→the number and position of nearest-neighbor atoms => large numbers of nearest neighbors and dense atomic packings for metallic crystal structures.
METALLIC CRYSTAL STRUCTURES

## Slide 9
The Face-Centered Cubic Crystal (FCC) Structure
ex: Al, Cu, Au, Pb, Ni, Pt, Ag
a hard-sphere model for the FCC unit cell
Each corner atom contributes as 1/8.
There are 8 corner atoms in an FCC unit cell.
Each face atom contributes as 1/2.
There are 6 face atoms.
METALLIC CRYSTAL STRUCTURES

## Slide 10
The Face-Centered Cubic Crystal (FCC) Structure
Coordination number for FCC
METALLIC CRYSTAL STRUCTURES

## Slide 11
The Face-Centered Cubic Crystal (FCC) Structure
Atomic packing factor (APF) for FCC
a=4R => a =2R
Independent of R and a!
APF =
4
3
p
(
2
a/4
)
3
4
atoms
unit cell
atom
volume
a
3
unit cell
volume
=0.74
METALLIC CRYSTAL STRUCTURES

## Slide 12: Summary for FCC
METALLIC CRYSTAL STRUCTURES

## Slide 13
The Body-Centered Cubic (BCC) Crystal Structure
Each corner atom contributes as 1/8.
There are 8 corner atoms in
an FCC unit cell.
The center atom
contributes as 1.
There is only 1 center atom.
Ex: Cr, W, Fe (), Ta, Mo,etc.
METALLIC CRYSTAL STRUCTURES

## Slide 14
The Body-Centered Cubic (BCC) Crystal Structure
Coordination number for BCC
Total 8 nearest neighbor atoms
Coordination number = 8
METALLIC CRYSTAL STRUCTURES

## Slide 15
Atomic packing factor (APF) for BCC
APF =
4
3
p
(
3
a/4
)
3
2
atoms
unit cell
atom
volume
a
3
unit cell
volume
length = 4R =
Close-packed directions:
3 a
=0.68
METALLIC CRYSTAL STRUCTURES

## Slide 16: Summary for BCC
METALLIC CRYSTAL STRUCTURES

## Slide 17
Hexagonal Close-Packing (HCP) Crystal Structure
• Coordination # = 12
• ABAB... Stacking Sequence
• APF = 0.74
• 3D Projection
• 2D Projection
6 atoms/unit cell
• c/a = 1.633
c
a
A sites
B
sites
A sites
Bottom layer
Middle layer
Top
layer
The top and bottom faces of the unit cell consist of six atoms that form regular hexagons and surround a single atom in the center.
METALLIC CRYSTAL STRUCTURES
• a = 2R
Ti, Mg, Zn, Co, Cd, Zr, Be
• V = a2 × c × cos 30°
12×(1/6) + 2×(1/2) + 3 =
Notes: The coordination number and the atomic packing factor for the HCP crystal structure
are the same as for FCC: 12 and 0.74, respectively

## Slide 18
DENSITY COMPUTATIONS
where n = number of atoms/unit cell
A = atomic weight
VC = Volume of unit cell = a3 for cubic
NA = Avogadro’s number
= 6.022 x 1023 atoms/mol
Density =  =
Cell
Unit
of
Volume
Total
Cell
Unit
in
Atoms
of
Mass
A knowledge of the crystal structure of a metallic solid permits computation of its theoretical density through the relationship;
METALLIC CRYSTAL STRUCTURES

## Slide 19: EXAMPLE PROBLEM: Theoretical Density, r
Cr (BCC) A = 52.00 g/mol R = 0.125 nm compute its theoretical density and compare the answer with its measure
theoretical
a = 4R/ 3 = 0.2887 nm
ractual
a
R
= 7.18 g/cm3
= 7.19 g/cm3
Adapted from
Fig. 3.2(a), Callister & Rethwisch 8e.
n = 2 atoms/unit cell

## Slide 20: Densities of Material Classes
r
metals
>
r
ceramics
>
r
polymers
Why?
Data from Table B.1, Callister & Rethwisch, 8e.
r
(g/cm )
3
Graphite/
Ceramics/
Semicond
Metals/
Alloys
Composites/
fibers
Polymers
1
2
2
0
30
B
ased on data in Table B1, Callister
*GFRE, CFRE, & AFRE are Glass,
Carbon, & Aramid Fiber-Reinforced
Epoxy composites (values based on
60% volume fraction of aligned fibers
in an epoxy matrix).
10
3
4
5
0.3
0.4
0.5
Magnesium
Aluminum
Steels
Titanium
Cu,Ni
Tin, Zinc
Silver, Mo
Tantalum
Gold, W
Platinum
G
raphite
Silicon
Glass
-
soda
Concrete
Si nitride
Diamond
Al oxide
Zirconia
H
DPE, PS
PP, LDPE
PC
PTFE
PET
PVC
Silicone
Wood
AFRE
*
CFRE
*
GFRE*
Glass fibers
Carbon
fibers
A
ramid fibers
Metals have...
• close-packing
(metallic bonding)
• often large atomic masses
Ceramics have...
• less dense packing
• often lighter elements
Polymers have...
• low packing density
(often amorphous)
• lighter elements (C,H,O)
Composites have...
• intermediate values
In general

## Slide 21: POLYMORPHISM AND ALLOTROPY
Some metals, as well as nonmetals, may have more than one crystal structure, a phenomenon known as polymorphism.
When found in elemental solids, the condition is often termed allotropy.
The prevailing crystal structure depends on both the temperature and the external pressure. Physical properties and density change during polymorphic transformations.
Example I: Carbon;
Graphite is the stable polymorph at ambient conditions
Diamond is formed at extremely high pressures
Example III: tin- “tin disease.”
Gray tin
White tin
The rate at which this change takes place is extremely slow!!! However could be faster at lower temperatures!!!
Vol 27% ↑; density↓ (from 7.30 g/cm3 (white) to 5.77 g/cm3 (gray).
Example II: Iron;
BCC at room temperature
FCC at 912 °C
Body-centered tetragonal  cubic

## Slide 22: CRYSTAL SYSTEMS
The unit cell geometry is completely defined in terms of six parameters (lattice parameters of a crystal structure):
-the three edge lengths a, b, and c,
the three interaxial angles ,  , and .
On this basis there are seven different possible combinations of a, b, and c, and , ,
and  , each of which represents a distinct crystal system.
These seven crystal systems are cubic, tetragonal, hexagonal, orthorhombic, rhombohedral (trigonal), monoclinic, and triclinic.

## Slide 23
The cubic system, for which a =b =c and a= b= g 90, has the greatest degree of symmetry.
The least symmetry is displayed by the triclinic system, because a≠b ≠ c and a ≠ b ≠ g .

## Slide 24: Crystallographic Points, Directions, and Planes
When dealing with crystalline materials, it often becomes necessary to specify a particular point within a unit cell, a crystallographic direction, or some crystallographic plane of atoms.

## Slide 25: a) Point Coordinates
Crystallographic Points, Directions, and Planes
to define a point within a unit cell….
Essentially same as Cartesian coordinates except values of x, y, and z
are expressed as fractions of the magnitude of unit vector(s) (and x, y,
and z not necessarily orthogonal).
not to separate these coordinates by commas or any other punctuation marks!!!

## Slide 26: b) Crystallographic Directions
Crystallographic Points, Directions, and Planes
1. Vector repositioned (if necessary) to pass
through origin. 2. Read off projections in terms of unit cell dimensions a, b, and c 3. Adjust to smallest integer values 4. Enclose in square brackets, no commas
[uvw]
ex: 1, 0, ½
=> 2, 0, 1
=> [ 201 ]
-1, 1, 1
families of directions <uvw>
z
x
Algorithm
y
A crystallographic direction is defined as a line between two points, or a vector.
where overbar represents a negative index
[ 111 ]
=>
if multiply by «–», [111] parallel but opposite direction

## Slide 27: b) Crystallographic Directions; Con’d
Crystallographic Points, Directions, and Planes
Note: for some crystal structures, different directions can be equivalent.
e.g. For cubic crystals:
are all equivalent
Angled brackets denote a family of crystallographic directions.

## Slide 28: Linear Density
ex: linear density of Al in [110] direction a = 0.405 nm
Linear Density of Atoms  LD =
a
[110]
Unit length of direction vector
Number of atoms
# atoms
length
1
3.5 nm
a
2
2
LD
-
=
=
Adapted from
Fig. 3.1(a),
Callister & Rethwisch 8e.
Linear density (LD) is defined as the number of atoms per unit length
the units of linear density are reciprocal length (e.g., nm-1, m-1).
if linear density of direction is same, the directions
are equivalent to each other.

## Slide 29: b) Crystallographic Directions; Con’d
Hexagonal Crystals
Crystallographic Points, Directions, and Planes
Coordinate axis system for a hexagonal unit cell
(Miller–Bravais scheme)
Directional indices, which are obtained as described earlier, will be denoted by four indices, as [uvtw]; by convention, the first three indices pertain to projections along the respective a1, a2, and a3 axes in the basal plane.
[010]  [1210]
-
-

## Slide 30: c) Crystallographic Planes
Crystallographic Points, Directions, and Planes
Algorithm
  1. Read off intercepts of plane with axes in
  terms of a, b, c
  2. Take reciprocals of intercepts
  3. Reduce to smallest integer values
  4. Enclose in parentheses, no
  commas i.e., (hkl)

## Slide 31: c) Crystallographic Planes
Crystallographic Points, Directions, and Planes
z
x
y
a
b
c
4. Miller Indices (110)
1. Intercepts
1 1 
2. Reciprocals
1/1 1/1 1/
1 1 0
3. Reduction
1 1 0
example
a b c

## Slide 32
z
x
y
a
b
c
4. Miller Indices (634)
example
1. Intercepts
1/2 1 3/4
a b c
2. Reciprocals
1/½ 1/1 1/¾
2 1 4/3
3. Reduction
6 3 4
c) Crystallographic Planes
Crystallographic Points, Directions, and Planes

## Slide 33
A “family” of planes contains all those planes that are crystallographically equivalent—that is, having the same atomic packing; and a family is designated by indices that are enclosed in braces—such as {100}
Family of planes, {100}, representing all faces of unit cells in the cubic system.
Family of planes
c) Crystallographic Planes
Crystallographic Points, Directions, and Planes

## Slide 34: PLANAR DENSITIES
Example:
  Draw (100) crystallographic planes
  for Fe.
  Calculate the planar density for each of these planes.
Planar density (PD) is taken as the number of atoms per unit area that are centered on a particular crystallographic plane
The units for planar density are reciprocal area (e.g., nm-2, m-2).

## Slide 35: Planar Density of (100) Iron
Solution: At T < 9120C iron has the BCC structure.
(100)
Radius of iron R = 0.1241 nm
R
3
3
4
a
=
Adapted from Fig. 3.2(c), Callister & Rethwisch 8e.
2D repeat unit
=
Planar Density =
a
2
1
atoms
2D repeat unit
=
nm2
atoms
12.1
m2
atoms
= 1.2 x 1019
1
2
R
3
3
4
area
2D repeat unit

## Slide 36: Crystalline and Noncrystalline Materials
SINGLE CRYSTALS:
For a crystalline solid, when the periodic and repeated arrangement of atoms is perfect or extends throughout the entirety of the specimen without interruption, the result is a single crystal.
All unit cells interlock in the same way and have the same orientation
http://iscrystals.com/contentimages/site/crystals.jpg
produced artificially
Naturally exist
Photograph of a garnet single crystal that was found in Tongbei, Fujian Province, China.
Within the past few years, single crystals have become extremely important in many of our modern technologies, in particular electronic microcircuits, which employ single crystals of silicon and other semiconductors.

## Slide 37: Crystalline and Noncrystalline Materials
2. POLYCRYSTALLINE MATERIALS:
Most crystalline solids are composed of a collection of many small crystals or grains; such materials are termed polycrystalline
small crystals or grains

## Slide 38
• atoms pack in periodic, 3D arrays
Crystalline materials...
-metals
-many ceramics
-some polymers
• atoms have no periodic packing
Noncrystalline materials...
-complex structures
-rapid cooling
crystalline SiO2
noncrystalline SiO2
"Amorphous" = Noncrystalline
Adapted from Fig. 3.23(b),
Callister & Rethwisch 8e.
Adapted from Fig. 3.23(a),
Callister & Rethwisch 8e.
Si
Oxygen
• typical of:
• occurs for:
Noncrystalline Materials

## Slide 39: Crystalline and Noncrystalline Materials
3. ANISOTROPY :
If the physical properties (the elastic modulus, the electrical conductivity, and the index of refraction, etc.) of single crystals of some substances depend on the crystallographic direction in which measurements are taken, this directionality of properties is termed as an anisotropy, associated with the variance of atomic or ionic spacing with crystallographic direction.
The extent and magnitude of anisotropic effects in crystalline materials are functions of the symmetry of the crystal structure;
e.i. the degree of anisotropy ↑ with ↓ structural symmetry—triclinic structures normally are highly anisotropic.
Substances in which measured properties are independent of the direction of measurement are isotropic.

## Slide 40: X-ray diffraction and Bragg’s Law
X-rays are a form of electromagnetic radiation with short wave-lengths and high energies.
For cubic symmetry:
n: order of reflection,
may be integer (1, 2, 3, etc..

## Slide 41: Example: For BCC iron, compute (a) the interplanar spacing, (b) the diffraction angle for the (220) set of planes. The lattice parameter for Fe is 0.2866 nm. Monochromatic radiation having a wavelength of 0.1790 nm is used, and the order of reflection is 1.
(a)
(b)